TECHNICAL INFORMATION

SCREEN - SOL Q T BLU

Codice: AM100013

APPLICATION FIELDS:

Flat printing. Resistant to water based inks plastisol, UV and solvent based inks.

GENERAL FEAUTURES

- Diazo-polymer emulsion blue.

- removable

- Solid content: 39%

- Pot life of the sensitized emulsion: 1

month

PREPARATION

Add water to diazo-sensitizer and shake well, then mix the whole dose with SCREEN-SOL Q T and let it settle for some time to eliminate air bubbles.

Since it is a polymer emulsion we recommend to work in an area with yellow light even before adding Diazo.

APPLICATION

We recommend to degrease the mesh . The ideal application is according to the mesh type, ink used and the RZ value that you want to obtain.

As a general indication, we suggest you to apply 1 or 2 coats of emulsion on the external face of the screen and 1 or 2 coats on the internal face, wet on wet.

DRYING

In ventilated oven, in horizontal, at 30-35°C for 40-60 minutes according  to the coating thickness .

EXPOSURE

Lamp type, distance from lamp to screen, mesh type and coating thickness can affect exposure time

To determinate the correct exposure time  we suggest to make some test with an exposure calculator.

Our suggestion:

Lighting halogen:		5000W

Application:			1-2 int. coats

1-2 ext. coats

Mesh 120.34 white		60 sec.

DEVELOPPING

Soak the screen in water for a few minutes or immediately apply a medium-pressure jet until the pattern has opened completely.

Then place in an oven to dry at 35°C.

CATALYSIS

The particolar formulation of SCREEN SOL Q T does not require the use of a catalyst, ensuring excellent resistance against all screen printing inks.

If you wish to further increase general resistance or if the printing environment is very humid, which could marginally affect the stencil’s resistance, we suggest you use SCREEN SOL CATALYST SPECIAL.

RECLAMING

The emulsion if not catalysed can be removed from the fabric. We recommend to remove accurately the ink with suitable products before reutilization. For this purpose you can use STRIP according to the instructions given in the product’s technical data sheet

POT-LIFE

If stored in its original container at a temperature between 15  and 25°C SCREEN SOL Q T will preserve its characteristics for at least 1 year from the date of production.

Amex srl gives the a/m suggestions as guidelines for the customer and assumes no liability direct or indirect for any improper use. It is the user's responsability to determine the suitability of the product to the intended use according to his working conditions.

Viale Dello Sport 12 - 22070 Appiano Gentile (CO) Tel. 031 931923