TECHNICAL INFORMATION

PLAST

Code: AM1200

PLAST PF

Without phtalate Code: AM1220

Plastisol ink suitable to print on t-shirt, sweater, etc. Available in 17 colours, 4 process colours and transparent.

GENERAL CHARACTERISTICS

- Highly opaque

- Good printability

- Bright colours

- High washing resistance at 60°C

PREPARATION

Ready to use. Check the viscosity according to the job.

PRINTING

To obtain best results use screens 34-90  threads/cm both for manual printing and automatic.

POLIMERIZATION

Using flash-dryers the printing process will be easier. To obtain washing resistance put in the oven at 160°C for 2-3 minutes.

ADDITIVES

PLAST ADDITIVO UP, to obtain puff effect (add 20% max)

PLAST ADDITIVO 66, to reduce viscosity, to increase brightness (add 5% max)

PLAST ADDENSANTE 740 to increase viscosity (add 0,3% 4 hours before the use)

PLAST ADDITIVO 378 to improve printability

(add 2% max)

PLAST ADDITIVO 24 to reduce viscosity and improve the printability (add max 1-2% max)

CLEANING

Wash tools with white spirit.

PACKING

5 – 20 KG.

NOTE

Before to use the ink in production, we suggest to make some test in order to evaluate if the product satisfies the requirement.

AVAILABLE COLOURS

Giallo limone 20, Giallo medio 22,Giallo caldo 23, Giallo extra,  Arancio 30, Scarlatto 39, Rosso vivo 41, Rosso Vivo extra, Rosso 40, Magenta 44, Viola 50, Verde Brillante 60, Azzurro 51, Blu royal 57, Blu navy 58, Oro 93, Oro brillante 90, Argento 91, Argento brillante, Nero 84, Nero extra 80, Bianco 10, Cyan quadricromia 73 Magenta quadricromia 72,Giallo quadricromia 71, Nero quadricromia 74, Pasta da taglio 03, Bianco flash e Bianco super.

Amex srl  gives the a/m suggestions as guidelines for the customer and assumes no liability direct or indirect for any improper use.

It is the  user’s responsibility to determine the suitability of the product to the intended use according to his working conditions.

Viale Dello Sport 12 - 22070 Appiano Gentile (CO) Tel. 031 931923