TECHNICAL INFORMATION

Gold / Silver Sparkle Plastisol

GENERAL CHARACTERISTICS

- Highly opaque

- Good printability

- Bright colours

- High washing resistance at 60°C

PREPARATION

Ready to use. Check the viscosity according to the job.

PRINTING

To obtain best results use screens 15 threads/cm (very coarse) both for manual printing and automatic.

POLIMERIZATION

Using flash-dryers the printing process will be easier. When printing a thicker deposit of ink please ensure you allow the entire ink to reach 160°. This special effect colour requires a coarse mesh so there is a thicker ink deposit. Sparkle colours will reflect the light and heat slightly so be aware it may need a slightly longer time to reach 160°.

ADDITIVES

PLAST ADDITIVO UP, to obtain puff effect (add 20% max)

PLAST ADDITIVO 66, to reduce viscosity, to increase brightness (add 5% max)

PLAST ADDENSANTE 740 to increase viscosity (add 0,3% 4 hours before the use)

PLAST ADDITIVO 378 to improve printability

(add 2% max)

PLAST ADDITIVO 24 to reduce viscosity and improve the printability (add max 1-2% max)

CLEANING

Wash tools with white spirit.

PACKING

5 – 20 KG.

NOTE

Before to use the ink in production, we suggest to make some test in order to evaluate if the product satisfies the requirement.

Amex srl  gives the a/m suggestions as guidelines for the customer and assumes no liability direct or indirect for any improper use.

It is the  user’s responsibility to determine the suitability of the product to the intended use according to his working conditions.

Viale Dello Sport 12 - 22070 Appiano Gentile (CO) Tel. 031 931923